## Slide 1: BT-7: Magnetic scattering in Ferromagnetic La0.7Sr0.3MnO3
David Lioi, Mitchell Bordelon, Kannan Lu,
Heda Zhang, Sharon S Philip, and Yuan Bo
NIST Center for Neutron Scattering
Summer School 2017

## Slide 2: (La3+)(Mn3+)O3 and (Sr2+)(Mn4+)O3
Zhao, Y.; Xu, Z.; Ratcliff, W.; Lynn, J. Magnetic Phase Transition and Spin Wave Excitations in the Colossal Magnetoresistive Manganites: An Experiment Using the BT7 Triple-Axis Spectrometer. NIST NCNR (2017).
Mn4+
FM conductor
t2g
eg
Δo
Mn3+
AFM insulator
Mn3+
O2-
Mn3+
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation

## Slide 3: (La3+)(Mn3+)O3 and (Sr2+)(Mn4+)O3
Mn4+
FM conductor
t2g
eg
Δo
Mn3+
AFM insulator
Mn3+
O2-
Mn4+
Zhao, Y.; Xu, Z.; Ratcliff, W.; Lynn, J. Magnetic Phase Transition and Spin Wave Excitations in the Colossal Magnetoresistive Manganites: An Experiment Using the BT7 Triple-Axis Spectrometer. NIST NCNR (2017).
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation

## Slide 4: (La3+)(Mn3+)O3 and (Sr2+)(Mn4+)O3
Charge, exchange, and geometry drive magnetic order
Mn4+
FM conductor
t2g
eg
Δo
Mn3+
AFM insulator
Mn3+
O2-
Mn4+
Zhao, Y.; Xu, Z.; Ratcliff, W.; Lynn, J. Magnetic Phase Transition and Spin Wave Excitations in the Colossal Magnetoresistive Manganites: An Experiment Using the BT7 Triple-Axis Spectrometer. NIST NCNR (2017).
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation

## Slide 5: La1-xSrxMnO3 at x=0.3
FM accompanies metal-insulator transition
Control with magnetic field
Colossal magnetoresistance
Resistivity change in magnetic field
Sample of interest:
La0.7Sr0.3MnO3
Insulator-Metal transition and giant magnetoresistance in La1-xSrxMnO3, A. Urushibara, Y. Motitomo, T. Arima, A. Asamitsu, G. and Y. Tokura, Phys. Rev. B 51, 14103 (1995)
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation

## Slide 6: BT-7 triple axis spectrometer
https://www.ncnr.nist.gov/instruments/bt7_new/PhotosofBT-7.html
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation

## Slide 7: BT-7 triple axis spectrometer
https://www.ncnr.nist.gov/instruments/bt7_new/
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation

## Slide 8: BT-7 triple axis spectrometer
TAS is ideally suited for probing small regions in k-space while varying an environmental parameter
(like temperature)
https://www.ncnr.nist.gov/instruments/bt7_new/PhotosofBT-7.html
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation

## Slide 9: Picking the E-k-space of Interest
T vs. Bragg peak intensity
Monitor magnetism with temperature
Align the crystal
Assess the strength of the magnetic order parameter
Extract useful physical constants
Magnetic Order Parameter
Critical
Fluctuations
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation

## Slide 10: Mapping out E-k-space of Interest
Inelastic scattering when Energy Transfer: E>0
Elastic scattering when energy transfer E=0
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation

## Slide 11: Model the Magnetic Dispersion
Plot the dispersion curve at each temperature
E=8|SJ|sin2(qa/2)~2|SJ|a2q2
Fit the experimental magnetic dispersion to the theoretical model in “SpinW” to extract the spin: J
JS= -3.56 meV
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation

## Slide 12: Acknowledgements
We in Group 2 would like to thank the scientists and staff at BT7 and at NCNR in general for putting on this school
Notes: 2d space integral over local magnetization
Magnetization field that begins orthonorm to plane and slowly turns over
Minimized with a circular orientation