## Slide 1: Measuring single chain dynamics in a polymer melt: from Rouse motion to entanglement distances
Apoorv Balwani, Shankar Ram, Saptarshi Chakraborty, Madhu Pallaka, Nicole Michenfelder-Schauser, Yuan Wei, Caitlyn Wolf
NCNR NIST Summer School 2017

## Slide 2
Bio compatible
Hydrophilic
Tunable mechanical properties
Drug delivery
Batteries
Poly(Ethylene Oxide) PEO

## Slide 3: Why are dynamics important?
Amorphous domains
Conduction mechanism in polymer electrolyte
Short length scales 0.1 nm
Long length scale >10nm
PEO
Tg = 213 K
Tm = 340K
Entanglement Mw =2 Kg/mol
Li+

## Slide 4: Rouse model
Shorter chains or smaller length scales
Reptation model
Longer chains or larger length scales
l
d
Dynamics models

## Slide 5
Dynamic crossover between different motions

## Slide 6
35 kg/mol PEO
Temperature: 400 K (> Tmelt = 340 K)
Rouse dynamics:
Time scale: < ~10 ns
Length scale: ~ 5.8 Å
(segment length)
Local reptation dynamics:
Time scale: > ~10 ns
Length scale: ~ 125 Å
(end-to-end distance)
Experimental details
Senses, E., Ansar, S.M., Kitchens, C.L., Mao, Y., Narayanan, S., Natarajan, B. and Faraone, A. Phys Rev Lett, 118 (2017).
Log G(t)
Log (t)
Glassy
α relaxation
Rubbery Plateau
Terminal
te
trep
t0

## Slide 7: Neutrons are perfectly situated to study polymer dynamics
Contrast matching
Strong force interaction
Notes: We all know that unlike x-rays, neutrons interact with the nuclei via the strong force instead of interacting with the electron cloud. This eliminates the strong dependence of scattering cross-section on atomic number and instead creates almost random scattering cross-sections. Contrast matching – deuterating most of the polymers and only some hydrogenated

## Slide 8
Parameter | Value
Neutron wavelength | 5-15 Å
Wavelength distribution (Δλ/λ) | 0.1 to 0.2
Energy resolution | ~ 10 neV
Rouse
Reptation
Neutrons are perfectly situated to study polymer dynamics
Notes: We all know that unlike x-rays, neutrons interact with the nuclei via the strong force instead of interacting with the electron cloud. This eliminates the strong dependence of scattering cross-section on atomic number and instead creates almost random scattering cross-sections. Contrast matching – deuterating most of the polymers and only some hydrogenated

## Slide 9
sample
Larmor precession frequency
Scattering of neutron beam provides dynamics information

## Slide 10
sample
Gif courtesy of Jülich NSE spectrometer facility
Scattering of neutron beam provides dynamics information

## Slide 11
sample
Gif courtesy of Jülich NSE spectrometer facility
Scattering of neutron beam provides dynamics information
Elastic scattering

## Slide 12
sample
Gif courtesy of Jülich NSE spectrometer facility
Scattering of neutron beam provides dynamics information
Inelastic scattering

## Slide 13
Local reptation dynamics:
Time scale: > ~ 10 ns
Length scale: ~ 125 Å
(end-to-end distance)
Contrast match: Mix 25% h-PEO and 75% d-PEO
Experimental details
75/25 d/h PEO
35 kg/mol PEO
Temperature: 400 K (> Tmelt = 340 K)
Rouse dynamics:
Neutron wavelength: 6 Å
Max Q: 0.3 Å–1
Rouse dynamics:
Time scale: < ~ 10 ns
Length scale: ~ 5.8 Å
(segment length)
Local reptation dynamics:
Neutron wavelength: 11 Å
Min Q: 0.05 Å–1

## Slide 14
Data Reduction
A
echo amplitude
normalized to static polarization count
Resolution is no
longer deconvolution…
Up
Down

## Slide 15
Results: Rouse dynamics
Wl4 = 1.391 ± 0.02254 nm4/ns

## Slide 16
Results: Reptation dynamics
d = 49.74 ± 0.68 Å

## Slide 17
Dynamic crossover between different motions
te = 47 ns

## Slide 18
Conclusions
Neutron spin echo provides longest time scale and length scale for dynamics measurements
Rouse and local reputation dynamics of complex systems can not be determined by other means (e.g. rheology)
Cross-over time between Rouse and local reptation modes can be calculated: 47 ns
 | Tube Diameter (Å) | τe (ns)
Niedzwiedz et al. ; 2008 | 49.74 | 47.3
Our Data | 52.6 | 51.2
T = 400 K

## Slide 19
Acknowledgments
Antonio Faraone
Elizabeth Kelly
Michi Nagao
Robert Bradbury
Erkan Senses
Guardians of the NSE
Alex Grutter
Rebecca Ogg
Yamali Hernandez
Arrangers: School of Neutrons
Last but in no way the least

## Slide 20
Thank you!

## Slide 21
td= 10 ^-7 s
Gplateau = 1.2 MPa

## Slide 22
Choice of wavelengths
2π/RE <Q = 2π/λ
0.05 Å-1< Q < 0.3 Å-1
10 ns

## Slide 23
Choice of wavelengths

## Slide 24
Polymer dynamics models modified to Fourier space & time
Modified Rouse model
Modified reputation model

## Slide 25
Number of precessions that neutrons go through
Here, Jmax = 0.5 T.m @ 400 Å
Jmin = 0.5/400 T.m @ 1 Å
The diffraction experiment
Chart: Q (Å-1)
| 0.05 | 0.06 | 7.0000000000000007E-2 | 0.08 | 0.09 | 0.1 | 0.11 | 0.12 | 0.13 | 0.14000000000000001 | 0.15 | 0.16 | 0.17 | 0.18 | 0.19 | 0.2 | 0.21 | 0.22 | 0.23 | 0.24 | 0.25 | 0.26 | 0.27 | 0.28000000000000003 | 0.28999999999999998 | 0.3
Total | 0.15439 | 0.11267 | 0.085715 | 0.06881 | 0.055702 | 0.046365 | 0.039221 | 0.034392 | 0.029486 | 0.026011 | 0.023645 | 0.020924 | 0.019293 | 0.017427 | 0.015832 | 0.014747 | 0.01358 | 0.012547 | 0.011935 | 0.011249 | 0.010557 | 0.010164 | 0.0096015 | 0.0092792 | 0.0090135 | 0.0085318
Up | 0.15228 | 0.11015 | 0.082839 | 0.065696 | 0.052417 | 0.043049 | 0.035759 | 0.030972 | 0.026188 | 0.022461 | 0.020233 | 0.017354 | 0.015609 | 0.013965 | 0.012389 | 0.011099 | 0.0099526 | 0.0089271 | 0.0083761 | 0.0076771 | 0.0070852 | 0.0065642 | 0.0059929 | 0.0056356 | 0.0052594 | 0.0048484
Down | 0.0021103 | 0.0025197 | 0.0028756 | 0.0031138 | 0.0032852 | 0.0033164 | 0.0034617 | 0.0034204 | 0.0032989 | 0.0035495 | 0.0034118 | 0.00357 | 0.0036841 | 0.0034619 | 0.0034436 | 0.0036488 | 0.0036269 | 0.0036197 | 0.0035588 | 0.0035716 | 0.0034717 | 0.0036 | 0.0036085 | 0.0036437 | 0.0037541 | 0.0036834
Neutrons in magnetic field

## Slide 26
Table of output parameters
Parameters | Definition | Value | Unit
Segment length | l | 0.58 | nm
Rouse parameter | Wl4 | 1.31 | nm4/ns
Tube diameter | d | 4.974 | nm
Molar mass of monomer | Mo | 44 | g/mol
Total number of segments | N | 795 | -
Entanglements per chain | Mw/Me | 17.5 | -
End-to-end distance |  | 16.35 | nm
Radius of gyration |  | 6.678 | nm
Rouse diffusion coefficient |  | 0.0016 | nm2 /ns
Rouse time |  | 5543 | ns
Crossover time between Rouse and Reptation |  | 47.39 | ns
Reptation time |  | 180000 | ns
Reptation diffusion coefficient |  | 0.00024 | nm2 /ns
Parameters | Definition | Value | Unit
Segment length | l | 0.58 | nm
Rouse parameter | Wl4 | 1.31 | nm4/ns
Tube diameter | d | 4.974 | nm
Molar mass of monomer | Mo | 44 | g/mol
Total number of segments | N | 795 | -
Entanglements per chain | Mw/Me | 17.5 | -
End-to-end distance |  | 16.35 | nm
Radius of gyration |  | 6.678 | nm
Rouse diffusion coefficient |  | 0.0016 | nm2 /ns
Rouse time |  | 5543 | ns
Crossover time between Rouse and Reptation |  | 47.39 | ns
Reptation time |  | 180000 | ns
Reptation diffusion coefficient |  | 0.00024 | nm2 /ns

## Slide 27
Fundamental equations of NSE and output
Fourier time
Resolution taken with charcoal (high coherent signal, no dynamics)
Background is with empty can: Transmission fraction used for background subtraction

## Slide 28: Backup slides
Choice of wavelengths (time and length scales)
Equations
Table of calculated parameters
Fitting pol vs phase